| Safety | Very High, Fully Passive Safety systems | Very High, Fully Passive Safety systems | Very High, Fully Passive Safety systems | High but needing highly engineered safety systems |
| --- | --- | --- | --- | --- |
| Capital Costs | 1 to 3$/Watt | 2 to 3$/Watt | 3 to 4$/Watt | 4 to 6$/Watt |
| Resource Needs | 1 to 10 tonnes Thorium per GWe year | 20 to 40 tonnes Uranium per GWe Year plus 0.5 tonnes Thorium | 150 to 300 tonnes Uranium per GWe year | 250 tonnes Uranium per GWe year |
| Fuel Cycle costs | 0.2 to 0.5 cent/kwh All as capital costs of salt reprocessing which needs R&D | 0.1 cents/kwh No salt reprocessing, low uranium needs and no fabrication | 0.6 to 1 cents/kwh Roughly same uranium as PWR but more costly fabrication | 0.6 cents/kwh Includes uranium, enrichment and fabrication |
| Waste Profile | Virtually zero transuranic wastes so only 300 year sequestration for fission products | Small fraction the transuranics of PWR or virtually zero if batch recycle every 10 years | Only Once Through Cycle appears economic so same profile as PWR | 250 kg per GWe year of transuranic waste (Pu etc), 100,000 year sequestration |
| Ability to burn off existing nuclear wastes (Pu) | Yes completely | Yes completely | Only partially | Only partially, MOX only transmutes half the Pu and no other transuranics |
| Industrial Heat applications and/or Hydrogen Production | Yes, 700 C heat output enormous potential uses including high temperature electrolysis, oil refining, oil sands | Yes, 700 C heat output | Yes, 700 C heat output | 300 C output so only very limited heat applications |
| Efficiency and Cooling Requirements | About 50% thermal efficiency and dry cooling capable. Many attractive power cycles (Steam, CO2, Air) | About 50% thermal efficiency and dry cooling capable (Steam, CO2, Air) | About 50% thermal efficiency and dry cooling capable (Steam, CO2, Air) | 35% efficiency limited to “wet” steam turbines and must reject far more heat. Dry cooling uneconomical |

# Text boxes

MSR Tube Within Tube Breeder

“The Luxury Model”,

More R&D to develop but bigger rewards

DMSR Converter

“The Work Horse”

Not as sexy but has everything needed with little R&D and low costs

Molten Salt “cooled” Reactors

“The compromise” More acceptable to traditional nuclear engineers but less payoff

Pressurized Water Reactor

“The Technology Lock In”  Head start as best fit for a submarine.  Little room for improvement